## Slide 1: CHAPTER 4
Solidification
and
Crystalline Imperfections

## Slide 2
Ni-based Superalloy Dendrites
The solidification of the alloy takes place over a range of tempt.
A pasty form that consists of tree-like solid structures (dendrite) and liquid metal.
L  L + S (Dendrites)  S (Grains)

## Slide 3
Semicontinuously Cast Al-ingot
Metals are melted to produce finished and semi-finished parts.
Fig. 4.1: Large, semicontinuously cast aluminum alloy ingot being removed from casting pit 鑄坑. Ingot of this type are subsequently hot- and cold-rolled into plate or sheet.

## Slide 4: Solidification of Metals
Two steps of solidification
    Nucleation: Formation of stable nuclei.
    Growth of nuclei: Formation of grain structure.
Thermal gradients define the shape of each grain.
Liquid
Nuclei
Crystals that will
Form grains
Grain Boundaries
Grains

## Slide 5
Fig. 4.3 A grain grouping parted from an arc-cast titanium alloy ingot under the blows of a hammer. The grouping has preserved the true bonding facets of the individual grains of the original cast structure. The grains are equiaxed since their growth is about equal in all direction.
Cast Grain Structure of Ti

## Slide 6: Formation of Stable Nuclei
Two main mechanisms: Homogenous and Heterogeneous.
Homogenous Nucleation:
    First and simplest case.
    Metal itself will provide atoms to form nuclei.
    Metal, when significantly undercooled, has several slow moving atoms which bond each other to form nuclei.
    Cluster of atoms below critical size is called embryo.
    If the cluster of atoms reach critical size, they grow into crystals. Else get dissolved.
    Cluster of atoms that are grater than critical size are called nucleus.
胚核
核，晶核

## Slide 7: Homogenous Nucleation均質孕核
Volume Free Energy ΔGV
Released by liquid to solid transformation.
ΔGv is change in free energy per unit volume between liquid and solid.
Free energy change for a spherical nucleus of radius r is given by
Surface Energy ΔGS
Required to form new solid surface
ΔGS is energy needed to create a surface.
γ is specific surface free energy.
Then
ΔGS is retarding energy.

## Slide 8
Homogenous Freezing Data
熔化熱
最大過冷

## Slide 9: Total Free Energy Change
Total free energy is given by
Nucleus
Above critical
radius r*
Below critical
radius r*
Energy
lowered by
growing into
crystals
Energy
lowered by
redissolving
When r = r*, d(ΔGT)/dr = 0 
r*
r
ΔG
+
-
ΔGV
ΔGS
ΔGT
r*

## Slide 10: Critical Radius Versus Undercooling
Greater the degree of undercooling, greater the change in volume free energy ΔGV.
ΔGS does not change significantly.
As the amount of undercooling ΔT increases, critical nucleus size decreases.
Critical radius is related to undercooling by relation
r* = Critical radius of nucleus
γ = Surface free energy
ΔHf = Latent heat of fusion
ΔT = Amount of undercooling.

## Slide 11
Critical Cu Radius Versus T
5 nm
胚核
晶核

## Slide 12: Heterogeneous Nucleation
Nucleation occurs in a liquid on the surfaces of structural material. e.g.: Container surface, Insoluble impurities.
These structures, called nucleating agents, lower the free energy required to form stable nucleus.
Nucleating agents also lower the critical size.
Smaller amount of undercooling is required to solidify. 0.1-10 K vs. 100-300 K. Used excessively in industries.

## Slide 13: Growth of Crystals and Grain Structure
Nucleus grow into crystals in different orientations.
Crystal boundaries are formed when crystals join together at complete solidification.
Crystals in solidified metals are called grains. Polycrystalline.
Grains are separated by grain boundaries.
More the number of nucleation sites available, more the number of grains formed.
Coarse grain vs. fine grain
Nuclei growing into grains
forming grain boundaries
多晶

## Slide 14: Types of Grains
Equiaxed Grains等軸晶:
    Crystals, smaller in size, grow equally in all directions.
    Formed at the sites of high concentration of the nuclei.
    Example: Cold mold wall (Large undercooling)
Columnar Grains柱狀晶:
    Long thin and coarse.
    Grow predominantly in one direction.
    Formed at the sites of slow cooling
    and steep temperature gradient.
    Example: Grains that are away from the mold wall.
Columnar Grains
Equiaxed Grains
Mold

## Slide 15
Solidification Structure
Fig. 4.7 (a) Schematic drawing of a solidification metal grain structure produced by using a cold mold. (b) Transverse section through an ingot of Al-1100 (99.0% Al).

## Slide 16: Casting in Industries
In industries, molten metal is cast into either semi finished or finished parts.
Forgings vs. Casting
Sheet ingot板鑄錠vs. Extrusion billet擠錠
In the steel industry, 60%: Stationary molds; 40%: Continuous casting.
Direct-Chill semicontinuous
casting unit for aluminum
Iron Smelting: Video

## Slide 17
Continuous Casting
Slab or Stripe 厚坯或薄片

## Slide 18: Grain Structure in Industrial Castings
To produce cast ingots with fine grain size, grain refiners are added. Fine dispersion of heterogeneous nuclei.
Example: For aluminum alloy, small amount of Titanium, Boron or Zirconium is added.
(a)
(b)
Grain structure of
Aluminum cast
(0.15-m-diameter extrusion ingot) without (a) and
with (b) grain refiners.
晶粒細化劑

## Slide 19: Solidification of Single Crystal
For some applications (e.g.: Gas turbine blades-high temperature environment), single crystals are needed.
Single crystals have high temperature creep resistance.
Latent heat of solidification is conducted through solidifying crystal to grow single crystal.
Growth rate is kept slow so that temperature at solid-liquid interface is slightly below melting point.
(a) Equiaxed grain vs. (b) Columnar grain vs. (c) Single crystal
氣渦輪葉片
抗潛變

## Slide 20
Fig. 4.12 Growth of single crystal for turbine airfoil渦輪翼片.
Starter with a pigtail
(single -crystal selector)
Producing a Single Crystal
選晶器

## Slide 21: Czochralski Process
This method is used to produce high-quality single crystal of silicon for IC wafers.
A seed crystal is dipped in molten silicon and rotated.
The seed crystal is withdrawn slowly while silicon adheres to seed crystal and grows as a single crystal (12”).
種晶

## Slide 22: Metallic Solid Solutions
Pure form: 99.99% Cu for electronic wires, 99.99% Al for decorative proposes (very bright metallic surface).
Alloys are used in most engineering applications: higher strength, corrosion resistance….
Alloy is an mixture of two or more metals and nonmetals.
Example:
    Cartridge brass is binary alloy of 70% Cu and 30% Zinc.
    Inconel 718 is a nickel based superalloy with 7 elements (50~55Ni-17~21Cr-4.75~5.50(Nb+Ta)-Balance Fe-2.8~3.3Mo-0.65~1.15Ti-0.20-0.80Al-<1.0Co-<0.08C-<0.015P….)
Solid solution (固溶體) is a simple type of alloy in which elements are dispersed in a single phase. Substitutional or Interstitial solid solution.
炮管黃銅
取代型或填隙型

## Slide 23: Substitutional Solid Solution
Solute atoms substitute for parent solvent atom in a crystal lattice.
The structure remains unchanged.
Lattice might get distorted due to change in diameter of the atoms.
Solute percentage in solvent can vary from a fraction of an atomic percent to 100%.
Solvent atoms
Solute atoms
(111) of FCC

## Slide 24: Substitutional Solid Solution (Cont..)
Hume-Rothery rules: The solubility of solids is greater if
    The diameter of atoms not differ by more than 15%.
    Crystal structures are the same.
    No appreciable difference in electronegativity (else compounds will be formed).
    Have same valence.
Examples:
System | Atomic radius difference | Electro- negativity difference | Maximum solid solubility
Cu-Zn | 3.9% | 0.1 | 38.3 at%
Cu-Pb | 36.7% | 0.2 | 0.17 at%
Cu-Ni | 2.3% | 0 | 100 at%
Cu-Si | 8.6% | 0 | 11.2 at%

## Slide 25: Interstitial Solid Solution
Solute atoms fit in between the voids (interstices) of solvent atoms.
Solvent atoms in this case should be much larger than solute atoms.
Example: between 1185 and 1667 K, interstitial solid solution of carbon in γ iron (FCC) is formed.
A maximum of 2.08 wt% (FCC, 1421 K) or 0.025 wt% (BCC, 996 K) of carbon can dissolve interstitially in iron.
Carbon atoms r = 0.075 nm
Iron atoms r = 0.129 nm
FCC voids = 0.053 nm
(BCC voids = 0.036 nm)
(100) of FCC -Fe

## Slide 26: Crystalline Imperfections
No crystal is perfect.
Imperfections affect mechanical properties, chemical properties and electrical properties.
Imperfections can be classified as
    Zero dimensional or point defects.
    One dimensional or line defects (dislocations).
    Two dimension defects (surfaces, grain or twin boundaries).
    Three dimension defects (pores, inclusions, cracks).
差排
雙晶
介在物

## Slide 27: Point Defects – Vacancy
Vacancy is formed due to a missing atom.
Vacancy is formed ( 1 vacancy/10000 atoms) during crystallization or mobility of atoms.
Also caused due to plastic deformation, rapid cooling or particle bombardment.
Energy of formation is about 1 eV.
Mobility of vacancy results in cluster of vacancies. Divacancies, Trivacancies.
Vacancies can move by exchanging positions with their neighbors (Diffusion).
空位
擴散

## Slide 28: Point Defects - Interstitialcy
Interstitialcy (Self-interstitial): Atom in a crystal occupies interstitial site.
This does not occur naturally. Can be induced by irradiation.
This defect caused structural severe distortion.

## Slide 29: Point Defects in Ionic Crystals
Complex as electric neutrality has to be maintained.
If two oppositely charged particles are missing, cation-anion divacancy is created. This is Scohttky imperfection.
Frenkel imperfection is created when cation moves to interstitial site.
These defects increase their electrical conductivity.
Impurity atoms are also considered as point defects.
Si + a few impurity  resistivity 

## Slide 30: Line Defects – (Dislocations)
Lattice distortions are centered around a line.
Formed during
      Solidification
      Permanent or plastic deformation
      Vacancy condensation
Different types of line defects are
      Edge dislocation
      Screw dislocation
      Mixed dislocation

## Slide 31
Edge Dislocation
Created by insertion of extra half planes of atoms.
: Positive edge dislocation; : Negative edge dislocation
Burgers vector (slip) b shows displacement of atoms.
Burgers vector b

## Slide 32
Strain Fields of Dislocations
Edge Dislocation
Screw Dislocation

## Slide 33: Screw Dislocation
Created due to shear stresses applied to regions of a perfect crystal separated by cutting plane.
Distortion of lattice in form of a spiral ramp.
Burgers vector is parallel to dislocation line.
6
6
6
6

## Slide 34: Mixed Dislocation
Most crystal have components
of both edge and screw
dislocation.
Dislocation, since irregular atomic arrangement will appear as dark lines when observed in electron microscope.
Dislocation structure of iron deformed 14% at –195 C
Mixed

## Slide 35: Planar Defects
Free surfaces, grain boundaries, twins雙晶, low angle boundaries, twists 扭旋 and stacking faults 疊差.
Free surface is the most common type: Bonded to atoms on only one side and hence has higher state of energy. Highly reactive (corrosion, reaction)
Nanomaterials have small clusters of atoms and hence are highly reactive.

## Slide 36: Grain Boundaries
Formed due to simultaneously growing crystals meeting each other. Grain boundaries separate grains.
Width = 2-5 atomic diameters. Atomic packing is lower.
Atoms in grain boundaries have higher energy.
Grain boundaries: Restrict plastic flow and prevent dislocation movement. Nucleation sites, Rapid diffusion region.
3D view of
grains
Grain boundaries
in 1018 steel

## Slide 37: Twin Boundaries
Twin: A region in which mirror image of the structure exists across a boundary.
Formed during plastic deformation (deformation twin) and recrystallization 再結晶 (annealing 退火 twin).
Twin boundaries form in pairs.
Strengthens the metal.
Twin
Twin Plane

## Slide 38
Annealing Twins
Fig. 4.23 Twin boundaries in the grain structure of brass.

## Slide 39: Other Planar Defects
Small angle boundary: Array of dislocations tilts (edge disl.) or twists (screw disl.) two regions of a crystal by < 10; high energy and strengthen.
Stacking faults: Piling up faults during crystal growth, collapse of vacancies, disl. interaction.
    ABCABABCABC…(FCC fault); ABABCABAB…(HCP fault)
Volume defects: Cluster of point defects join to form 3-D void. Three dimensional precipitates or inclusions. Tremendous effect on the behavior of the materials.

## Slide 40
Optical Metallography金相
Microstructure Analyses: OM, SEM, TEM, HRTEM, STM.
To observe grain boundaries, the metal sample must be first mounted for easy handling.
Then the sample should be ground and polished with different grades of abrasive paper and abrasive solution.
The surface is then etched chemically.
Tiny groves are produced at grain boundaries.
Groves do not intensely reflect light. Hence observed by optical microscope.
Impurities, Phases, Defects….

## Slide 41: Effect of Etching 蝕刻
Unetched
Steel
200
Etched
Steel
200
Unetched
Brass
200
Etched
Brass
200

## Slide 42
Grain Boundaries (OM)
Fig. 4.27 Grain boundaries on the surface of polished and etched samples as revealed in the optical microscope. (a) Low-carbon steel, 100. (b) Magnesium oxide, 225

## Slide 43: Grain Size
Grain size affects the mechanical properties of the material.
The smaller the grain size, more are the grain boundaries.
More grain boundaries means higher resistance to slip (plastic deformation occurs due to slip) and strengthens metals.
At elevated temperature, grain boundary sliding may occur, and grain boundaries can become regions of weakness in polycrystalline metals.
ASTM grain size number ‘n’ is a measure of grain size.
N = 2n1
n < 3 – Coarse grained
4 < n < 6 – Medium grained
7 < n < 9 – Fine grained
n > 10 – Ultrafine grained
N = Number of grains per square 2.54  102 m of a polished and specimen at 100 .
n = ASTM grain size number.

## Slide 44
200 
200 
1018 cold rolled steel, n = 10
1045 cold rolled steel, n = 8
m 226 160 113 80 57 40 28 20 14 10

## Slide 45
Grain Size (Cont..)
Fig. 4.28 Several nominal ASTM grain sizes of low-carbon steels: (a) n = 7, (b) n = 8, and (c) n = 9.

## Slide 46: Average Grain Diameter
Average grain diameter more directly represents grain size.
Random line of known length is drawn on photomicrograph.
Number of grains intersected is counted.
Ratio of number of grains intersected to length of line, nL is determined.
10 grains / 100 mm 225.
1
6
10
C = 1.5, and M is
magnification
d = C/(nLM)
d = 1.5  10 mm / 225 = 6.7  102 mm = 67m

## Slide 47: Scanning Electron Microscope
Electron source generates electrons. W, LaB6, FE
Electrons hit the surface and secondary electrons are produced.
The secondary electrons are collected to produce the signal.
The signal
is used to
produce
the image.
SEM of fractured metal end
場發射
掃描式電子顯微鏡(SEM)

## Slide 48
Depth of field 景深: 300 times that of OM. 10 m at 10,000
Magnification: 15 -500,000
The samples are often coated with Au or C especially for nonconducting materials.
Chemical analysis: SEM is always equipped with an X-ray spectrometer.
Scanning Electron Microscope (Cont…)
Fig. SEM fractograph of intergranular corrosion fracture near a circumferential weld in a thick-wall tube made of type 304 stainless steel.

## Slide 49: Transmission Electron Microscope
Electron produced by heated tungsten filament.
Accelerated by high voltage (75-300 kV)
Electron beam passes through very thin specimen.
Difference in atomic arrangement change directions of electrons.
Beam is enlarged and focused on fluorescent screen.
Bright field vs. Dark field images.
Collagen Fibrils
膠原纖維 of ligament 韌帶 as seen in TEM
穿透式電子顯微鏡(TEM)
投射鏡
中間鏡
物鏡
聚焦鏡
試樣

## Slide 50
TEM (Cont…)
TEM needs complex sample preparation.
Electropolishing, ion-beam thinning, and focus ion beam (FIB).
Very thin specimen needed ( several hundred nanometers)
Magnification: 50 -1,500,000
Diffraction and chemical analysis.
聚焦離子束

## Slide 51
TEM and HRTEM Images
Fig. 4.33 TEM bright field image shows dislocation structure in iron deformed 14% at 78 K.
Fig. 4.34 HRTEM image of AlN atomic structure. Dislocation: d Stacking fault: two opposing arrows.
高解析穿透式電子顯微鏡(HRTEM)

## Slide 52
High resolution TEM (HRTEM) allows resolution of 0.1 nm, atomic level.
The sample must be significantly thinner—on the order of 10-15 nm.
2-D projections of a crystal with accompanying defects can be observed.
The thin sample is tilted so that a low-index direction in the plane is perpendicular to the direction of electron beam.
Dislocations create a wavy pattern in atomic structure.
High-Resolution TEM

## Slide 53: Scanning Probe Microscopy (SPM)
SPM: Scanning Tunneling Microscope (STM) and Atomic Force Microscope (AFM).
Sub-nanometer magnification.
Atomic scale topographic map of surface.
STM uses extremely sharp tip (W, Ni, Pt-Ir or carbon nanotubes).
Fig. 4.35 STM tip made of Pt-Ir alloy. The tip is sharpened using chemical etching techniques.
掃描穿隧顯微鏡
原子力顯微鏡
掃描探針顯微鏡

## Slide 54: Scanning Tunneling Microscope
Tip placed one atom diameter from surface.
Voltage applied across tip and surface.
Electrons tunnel the gap and produce current.
Current produced is proportional to change in gap.
Can be used only for conductive materials.
Constant current mode Constant height mode

## Slide 55
Surface of platinum with defects
Fig. 4.37 STM image of the surface of platinum showing outstanding atomic resolution.
STM Images

## Slide 56: Atomic Force Microscope
Similar to STM but tip attached to cantilever beam.
When tip interacts with surface, van der Waals forces deflect the beam.
Deflection detected by laser and photodetector.
Short-range repulsive force (contact mode) vs. Long-range attractive force (non-contact mode)
Non-conductive materials can be scanned.
Used in DNA research and polymer coating technique.
懸臂樑

## Slide 57
Summary
Metals: Melted and cast into ingots or parts.
Solidification  Polycrystalline grain  Grain size.
ASTM grain size number n or average grain diameter.
Large Si single crystals are used in IC industries and this Si must be of very high purity.
Crystal Imperfections: Point defects: vacancies, solutes. Line defects: edge and screw dislocations. Two-dimensional defects: surfaces, internal boundary. Three-dimensional defects: pores, inclusions, cracks.
Microstructure Analysis: OM, SEM, TEM, HRTEM, STM, AFM.